The intriguing effect of thiolates as co-ligands in platinum(II) complexes bearing a cyclometalated 1,3-di(2-pyridyl)benzene

Francesco Fagnani,a,* Alessia Colombo,a Claudia Dragonetti,a Dominique Robertoa and Daniele Marinottob

a Dipartimento di Chimica dell’Università degli Studi di Milano and UdR di Milano dell’INSTM, via Golgi 19, Milano, Italy; francesco.fagnani@unimi.it

b CNR-SCITEC, Institute of Chemical Science and Technologies “Giulio Natta”, via Corti 12, Milano, Italy.

Dedicated to Professor Renato Ugo, a great scientist and an exceptional guide full of humanity

Keywords: Platinum(II) complexes, phosphorescence, thiolate

Abstract

Substitution of the chlorido ligand of the fascinating cyclometalated complex [Pt(5-mesityl-1,3-di(2-pyridyl)benzene)Cl] by thioacetate leads to the related thiolato complex [Pt(5-mesityl-1,3-di(2-pyridyl)benzene)(thioacetate)], which has been fully characterised. Its photophysical properties were determined in degassed dichloromethane solution, as blend in Poly(MethylMethAcrylate) (PMMA) thin films, and as powders, at room temperature. Both in solution and in thin films, an increase of the concentration of the complex leads to a red shift of the phosphorescence spectra and to a decrease of lifetime decays and quantum yield. It appears that tuning of emission spectra depends on the competition between monomeric and aggregate emissive states. No clear evidence of excimer formation has been detected. In powders, an aggregate emission spectrum is red-shifted at 602 nm, reaching a very low phosphorescence quantum yield of 1 %.

1. Introduction

In the last decades, cyclometalated platinum(II) complexes have attracted considerable interest in a wide range of applications such as bioimaging [1-4], nonlinear optics [5-12], photodynamic therapy [13-15] and sensing devices [16-19]. They have also been applied as phosphorescent emitters in organic light-emitting diodes (OLEDs) exhibiting high emission efficiencies [20-31], due to the strong spin-orbital coupling which allows for efficient phosphorescence at room temperature [32]. Remarkably, the OLEDs emitted colour can be easily modulated by the concentration of the complex, as a consequence of the parallel emissions coming from the bi-molecular and mono-molecular excited states of the platinum complex [30]. The square planar geometry of platinum compounds allows the creation of bi-molecular states, either in the ground states (dimers) or in the excited states (excimers), by means of Pt-Pt and/or ligand-ligand intermolecular interactions [33]. Chlorido Pt(II) complexes bearing a cyclometalated 1,3-di(2-pyridyl)benzene (dpyb) are very bright emitters, with the monomer emission colour easily controlled upon introduction of suitable substituents on the pyridyl or phenyl rings of the cyclometalated N^C^N ligand [20]. For example, because the highest occupied molecular orbital (HOMO) is predominantly on platinum and on the benzene ring, whereas the lowest unoccupied molecular orbital (LUMO) is on the pyridines, the introduction of electron-accepting groups on the benzene (which decreases the HOMO energy) and electron-donating groups on the pyridines (which increases the LUMO energy) causes an increase of the HOMO-LUMO gap and consequently a blue shift of the emission. Vice-versa, introduction of electron-donating groups on the benzene ring or electron-accepting groups on the pyridines leads to a red-shift [20].

Surprisingly, the effect of the co-ligand on the photophysical properties of these fascinating N^C^N platinum complexes has not been well studied yet. Substitution of the chlorido ligand with an acetylide or isothiocyanate maintains high quantum yields (Φlum = 0.60-0.77) whereas Pt-OPh complexes have half the value of the quantum yields of the parent Pt-Cl complexes [30]. Seven years ago it was reported that replacement of the chlorido ligand by an electron-rich arenethiolate (SPhR) leads to much lower quantum yields (Φlum = 0.002-0.17 with respect to 0.58-0.60 for the chlorido derivative) and to a red-shift of the emission [34]. On the contrary, we recently found that [Pt(5-mesityl-dpyb)(1-phenyl-1H-tetrazole-5-thiolate)] (Fig. 1; complex 2) is characterized by a monomeric emission colour similar to that of the related chlorido complex, but it is much more emissive (Φlum = 0.90 with respect to 0.62 for the chlorido parent complex) [30]. This unexpected observation and the desire to gain a deeper understanding of the effect of sulphur co-ligands on the emission properties of [Pt(5-mesityl-dpyb)Cl] prompted us to investigate the use of another sulphur-donor ligand, i.e. thioacetate. Here we present the preparation, characterization, and photophysical properties at room temperature of the new complex [Pt(5-mesityl-dpyb)(thioacetate)] (Fig. 1; complex 1).

Figure 1. Structure of complexes [Pt(5-mesityl-dpyb)(thioacetate)] (1) and [Pt(5-mesityl-dpyb)(1-phenyl-1H-tetrazole-5-thiolate)] (2).

2. Experimental

2.1 Materials and methods

All reagents and solvents were purchased from Sigma-Aldrich and were used without further purification. The deuterated solvents for NMR measurements were purchased from Eurisotop.

Complex [Pt(5-mesityl-dpyb)Cl] was prepared by reaction of the N^C^N ligand with 1.2 eq of K2PtCl4 in glacial acetic acid at reflux under argon for 24 h, according to the literature [35].

Electronic absorption spectra were recorded at room temperature in CH2Cl2 solution, using a Shimadzu UV3600 spectrophotometer and quartz cuvettes with 1 cm optical path length.

Luminescence measurements were carried out in CH2Cl2 solution after three Freeze-Pump-Thaw cycles in order to remove dissolved oxygen. Absolute photoluminescence quantum yield (Φlum) was measured using a C11347 Quantaurus Hamamatsu Photonics K.K spectrometer.

Steady-state and time-resolved fluorescence data were obtained using a FLS980 spectrofluorimeter (Edinburg Instrument Ltd). A detailed description of the measurement techniques can be found in the SI.

2.2. Synthesis of [Pt(5-mesityl-dpyb)(thioacetate)]

Figure 2. Reaction scheme for the synthesis of the new complex 1.

[Pt(5-mesityl-dpyb)Cl] (70 mg, 0.121 mmol) was suspended in acetone (25 mL) and potassium thioacetate (166 mg, 1.45 mmol) was added. The obtained mixture was stirred at room temperature under argon atmosphere and in the dark. After 24 h the precipitation of an orange solid was observed. The desired product [Pt(5-mesityl-dpyb)(thioacetate)] was recovered by filtration, washed with acetone and diethyl ether, and dried (64 mg, 0.104 mmol, 86%).

1H NMR (400 MHz, CD2Cl2) δ (ppm): 9.34 (2H, d, J = 5.3 Hz, J(195Pt) = 45 Hz), 7.99 (2H, dd, J1 =7.8 Hz, J2 = 8.8 Hz), 7.71 (d, J = 7.8 Hz), 7.36-7.29 (4H, m), 7.01 (2H, s), 2.57 (3H, s), 2.37 (3H, s), 2.11 (6H, s).

13C NMR (100 MHz, CD2Cl2) δ (ppm):154.0, 139.2, 128.0, 123.5, 119.5, 37.3, 20.6, 20.5.

Anal. calcd for C27H24N2OPtS: C 52.33, H 3.90, N 4.52; found: C 52.46; H 3.92; N 4.54.

2.3. Preparation and characterization of blended PMMA thin films

Thin films containing 7.5 wt% and 15 wt% of [Pt(5-mesityl-dpyb)(thioacetate)] in poly-methylmethacrylate (PMMA, M̅w ≈15000 g/mol) on quartz plate (thickness 1 mm) were obtained by spin-coating (Cookson Electronic Company P-6708D). The parameters of spinning (RPM-revolutions per minute) were RPM 1: 800; Ramp 1: 1 s, Time 1: 5 s; RPM 2: 2000; Ramp 2: 1 s, Time 2: 60 s. The solution for the 7.5 wt% thin film was prepared with 10 mg of complex and 133 mg of PMMA in 7 ml of dichloromethane, while the solution for the 15 wt% thin film was prepared with 10 mg of complex and 66 mg of PMMA in 7 ml of dichloromethane.  The thickness, measured by an α-step stylus profilometer (DektaK XT, Bruker),  is 0.25 ± 0.02 μm and 0.16 ± 0.01 μm for the 7.5 wt% and 15 wt% thin films, respectively.

3. Results and discussion

The novel complex [Pt(5-mesityl-dpyb)(thioacetate)] was prepared by reaction of the related chlorido complex with potassium thioacetate (see Experimental). Its absorption spectra in dichloromethane at different concentrations are shown in Fig. 3. At dilute concentration, the absorption spectrum displays an intense absorption band at 260-320 nm (ε292 = 8.4103 L mol-1 cm-1) and a less intense band at 350-460 nm (ε391 = 2.2103 L mol-1 cm-1), as already observed for the parent chloride compound [35] and for its other derivative [Pt(5-mesityl-dpyb)(1-phenyl-1H-tetrazole-5-thiolate)] [30]; these bands can be assigned to intraligand 1π–π* transitions of the N^C^N ligand and to charge-transfer transitions involving the cyclometalated ligand and the metal, respectively [24]. When the concentration increases over 510-5 M, another absorption band with a peak at 490 nm becomes visible (inset in Fig. 3). This absorption band can be attributed to metal-to-ligand charge transfer 3π-π* transitions of the monomeric complex, as noted for other parent chloride derivatives [36]. However, superimposed to the latter, a wide and weaker absorption band in the range between 450 and 600 nm can be noted (inset of Fig. S2); this band increases with the solution concentration and therefore can be reasonably assigned to the formation of aggregates [30].

Figure 3. Absorption spectra of complex 1 in CH2Cl2 at different concentrations. The weak bands at longer wavelengths are shown on an expanded scale for clarity.

The [Pt(5-mesityl-dpyb)(thioacetate)] complex has also been studied in solid-state matrix as a blend in PMMA at two different concentrations in weight, 7.5 wt% and 15 wt%, respectively. The normalized absorption spectra of the two thin films are shown in Fig. 4; they are quite similar to those observed for the solutions at high concentration, in particular it is possible to notice more clearly the presence of an absorption band in the range between 450 and 600 nm which is more intense for the 15 wt% than for the 7.5 wt% Pt/PMMA thin film. This is consistent with a prominent solid-state aggregation behavior (due to the probable formation of dimers) as already observed for neat films of other square-planar Pt(II) complexes [33].

Figure 4. Normalized absorption spectra of the 7.5 wt% (red line) and 15 wt% (blue line) thin films of complex 1 in PMMA matrix.

Photoluminescence characterizations of the [Pt(5-mesityl-dpyb)(thioacetate)] complex were performed both in dichloromethane solution and in solid-state, as powders and as blend in PMMA. Relevant values are given in Tables 1 (solutions), 2 (powders) and 3 (thin films).

| Compound | λmax, abs / nm (ε / M-1 cm-1) | C / M | λmax em / nm (λex / nm) | QYafter | τ / µs | λex; λem / nm |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 241 (11.9·103) 292 (8.4·103) 391 (2.2·103) | 5·10-6 | 499 (390) | 0.23 | 0.34 (2.13%) 7.61 (97.87%) | 404; 498 |
|  |  |  |  |  | 0.30 (2.73%) 7.97 (97.27%) | 404; 620 |
|  |  | 2·10-4 | 499 (390) | 0.03 | 0.24 (50.25%) 3.10 (49.75%) | 404; 499 |
|  |  |  |  |  | 0.24 (60.49%) 3.25 (39.51%) | 404; 620 |
| 2 | 239 (34.8·103) 292 (24.6·103) 387 (5.2·103) | 1·10-6 | 498 (389) | 0.90 | 7.39 (100%) | 374; 498 |
|  |  | 2·10-4 | 498 (389) 650 (489) | 0.12 | 0.73 (72.11%) 2.43 (27.89%) | 374; 498 |

Table 1. Photophysical properties of complex 1 in dichloromethane solution and comparison with complex 2 [30]. QYafter refers to the absolute Quantum Yield measured after the Freeze-Pump-Thaw procedure.

| Compound | λmax em / nm | QY | τ/ µs | λex; λem / nm |
| --- | --- | --- | --- | --- |
| 1 | 601 | 0.01 | 0.05 (9.42%) 0.99 (90.58%) | 404; 597 |
| 2 | 703 | 0.62 | 1.24 | 374; 703 |

Table 2. Photophysical properties of complex 1 as powders and comparison with complex 2 [30].

| Compound | wt% in PMMA | λmax em / nm (λex / nm) | QY | τ/ µs | λex; λem / nm |
| --- | --- | --- | --- | --- | --- |
| 1 | 7.5 | 498 (391) 498 (430) 536 (470) | 0.17 | 1.08 (26.62%) 3.75 (73.38%) | 404; 500 |
|  | 15 | 499 (391) 502, 533 (450) 536 (470) | 0.10 | 0.66 (39.46%) 2.47 (60.54%) | 404; 500 |

Table 3. Photophysical properties of complex 1 at two different concentrations in PMMA thin films.

Absolute quantum yield (Φlum) measurements of the [Pt(5-mesityl-dpyb)(thioacetate)] complex at different concentrations in dichloromethane solution were carried out before and after three Freeze-Pump-Thaw (FPT) cycles. The Φlum of a diluted (510-6 M) solution after FPT is 0.23, which is lower with respect to that of both [Pt(5-mesityl-dpyb)Cl] (0.60) [24] and [Pt(5-mesityl-dpyb)(1-phenyl-1H-tetrazole-5-thiolate)] (0.90) [30]. As expected for Pt(II) complexes bearing a N^C^N ligand, the Φlum of the new complex measured before FPT is very low (0.047), showing that the emission is efficiently quenched by oxygen. Thus, the novel complex is a good sensor for oxygen and efficient production of singlet oxygen – i.e. the 1Δg state of O2 - can be anticipated.

The normalized emission and excitation spectra of [Pt(5-mesityl-dpyb)(thioacetate)] in diluted  and concentrated dichloromethane solutions are shown in Figg. S3, S4 and S5. The emission spectrum of the diluted (510-6 M) solution is highly structured, as expected for luminescence from states of primarily 3LC character, with a maximum at 498 nm, similar to that observed for the chloride parent compound and for the 1-phenyl-1H-tetrazole-5-thiolate derivative [24, 30]. Moreover, lifetime measurement of the complex (emission 498 nm, excitation 404 nm; Fig. S7) presents a bi-exponential decay with lifetimes of τ1 = 0.34 µs and τ2 = 7.61 µs, having a pre-exponential factor expressed as a percentage of 2.13% and 97.87%, respectively (Table 1). Such bi-exponential decay indicates the presence of multiple fluorophores within the solution [37], mostly monomers of the complex with a very low percentage of its aggregates. Neglecting the small presence of aggregates, we can assume that the excited state of the complex is formed with unitary efficiency and, considering the experimentally determined absolute QY and lifetime τ2, we can give an estimate of the radiative rate constant (kr = Φlum/τ2) and nonradiative rate constant (Σknr = τ2−1-kr) of the complex. Under this approximation, kr and knr have values of 3.02∙104 s-1 and 1.01∙105 s-1 respectively. A similar radiative rate constant is also observed for complex 2 in solution at concentration of 1∙10-5 M using the same approximation [30]. Attempts to compare more diluted solutions (e.g. 1∙10-6 M) of the new complex have failed, given the impossibility of measuring the absolute quantum at such low concentration.

In the case of [Pt(5-mesityl-dpyb)(thioacetate)], an increase of the concentration up to 1∙10-3 M leads to the appearance of a new small band around 530-600 nm (Fig. 5). This new band at lower energy, which changes in intensity by varying the excitation wavelength (Figg. S4 and S5), can be attributed to the emission from excited-state aggregates rather than to excimers, though the aggregates emission is not so red-shifted at higher wavelengths as for other Pt(II) complexes [38]. However, this assignment is supported by both the normalized excitation spectra, displaying a different shape compared to those obtained at more diluted concentration (Fig. S6), and by the study of solid-state photoluminescence (see below), in which a predominant aggregation emission is present in the same spectral region (530-650 nm). Therefore, no clear evidence of triplet excimer formation is observed for this complex in solution. In general, for Pt(II) complexes, the triplet excimer formation is attributable to the Pt-Pt and interligand π-π interactions [39]. In particular, Pt-Pt interactions are very critical and, when these are absent or are very weak, they do not lead to mentioned triplet excimer formation. In addition, the interligand π-π interactions also play a significant role in determining the magnitude of the HOMO-LUMO energy gap of the aggregates. Unfortunately, various attempts to grow single crystals of [Pt(5-mesityl-dpyb)(thioacetate)] have failed; therefore, it was not possible to obtain information on the  structure of the complex by X-ray crystallography. However, in the near future,  investigations by DFT calculations on the novel complex will be carried out with the aim of getting a better understanding of the Pt-Pt and  interactions.

As the concentration increases up to 2∙10-4 M, the absolute quantum yield decreases to 0.034 after three FPT cycles. In addition, lifetime measurements performed at 498 nm (Fig. S9) and 620 nm (Fig. S10) exciting at 404 nm still show a bi-exponential behavior (see Table 1). With respect to the more dilute solution, the first lifetime remains approximately the same, with a first pre-exponential factor of 50.25 % and 60.49 % at 498 nm and 620 nm, respectively; however, the second one decreases at around 3.10 ÷ 3.25 µs (Table 1). This behavior is compatible with an increase of aggregates.

Figure 5. Normalized emission spectra at 532 nm of complex 1 at different dichloromethane concentrations.

Photoluminescence measurements on powders were performed to probe more deeply the ability of [Pt(5-mesityl-dpyb)(thioacetate)] to form bi-molecular species (aggregates and/or excimers) and to study their nature.

The measured absolute quantum yield on powders of the complex is 0.01 (Table 2). This little value confirms that the aggregation of the molecules leads to a quenching of the luminescence, as already observed in solution when the concentration of the complex is increased.  Interestingly, the measured Φlum is much lower with respect to the powders of [Pt(5-mesityl-dpyb)(1-phenyl-1H-tetrazole-5-thiolate)] (0.62) [30]. Therefore, the use of thioacetate as donor ligand drastically alters the emissive properties of the complex in the solid-state.

The normalized emission and excitation spectra of the powders are shown in Fig. S16. The emission spectra present a little and structured phosphorescence at 500 nm (monomer emission) which is surmounted by a broader and more intense band with a maximum at 602 nm.  These two bands change their relative intensity by varying the excitation wavelength and, in addition, the excitation spectra collected at the emission wavelength of 503 nm and at 583 nm clearly display a different shape. Therefore, the broad and intense band can be attributed to the emission from excited-state aggregates, with no excimers formation observed in the powders of the complex. Lifetime measurement performed at 597 nm exciting at 404 nm gives a bi-exponential decay with a predominant lifetime of about 1.0 µs (see Fig. S17).

In addition, the luminescence properties of thin PMMA films of the complex were analyzed (data in Table 3). The measured absolute quantum yield on 7.5 wt% and 15 wt% thin films is 0.17 and 0.10, respectively. Thus, as the percentage in weight of the complex in PMMA increases, a quenching of the luminescence is observed. The emission spectra of both films display a structured phosphorescence at 500 nm, followed by a broader emission band at lower energy, (as can be seen in Figg. S11 and S13). As for the powders, the two bands change their relative intensity by changing the excitation wavelength. Moreover, the emission band at lower energy, which is more intense for the 15 wt% than for the 7.5 wt% thin film, overlaps quite well with the emission broad band observed for the powders (see Fig. 6). In addition, the excitation spectra collected at the emission wavelengths around 500 nm and 650 nm have a different shape; therefore the emission broad band that rises in the spectral region between 550 and 750 nm can be assigned to excited-state aggregates.

Figure 6. Normalized emission spectra (at 532 nm) of 7.5 wt%, 15 wt% thin films and powders of complex 1.

4. Conclusion

In conclusion, a novel complex, namely [Pt(5-mesityl-dpyb)(thioacetate)], was easily prepared and well characterized. In solution, its emission colour is similar to that of the parent chloride complex and of the similar derivative bearing an ancillary 1-phenyl-1H-tetrazole-5-thiolate. However, its luminescence quantum yield is lower, although it is much higher than that reported for related complexes with arylthiolates. In powder, a red-shift of the emission is observed, together with a strong quenching of the luminescence. For the 7.5 wt% and 15 wt% Pt/PMMA thin films, the emission is similar to that of the solution at high concentration, with a lower energy band which is more intense for the 15 wt% than for the 7.5 wt% thin film. It is still unclear how the nature of the thiolate affects the photophysical properties of the platinum(II) complexes based on a cyclometalating 1,3-di-(2-pyridyl)benzene. Our present results put in evidence how these families of compounds are really intriguing and merit to be deeply investigated. Therefore, there is a need for the preparation and characterization of platinum(II) complexes with other sulfur co-ligands, in order to understand the relationship between their nature and the emission properties of the compounds.

References

- E. Baggaley, J. A. Weinstein, J. A. G. Williams, Lighting the way to see inside the live cell with luminescent transition metal complexes, Coord. Chem. Rev., 2012, 256, 1762. DOI: 10.1016/j.ccr.2012.03.018

- E. Baggaley, S. W. Botchway, J. W. Haycock, H. Morris, I. V. Sazanovich, J. A. G. Williams, J. A. Weinstein, Long-lived metal complexes open up microsecond lifetime imaging microscopy under multiphoton excitation: from FLIM to PLIM and beyond, Chem. Sci., 2014, 5, 879. DOI: 10.1039/c3sc51875b

- M. Mauro, A. Aliprandi, D. Septiadi, N. S. Kehr, L. De Cola, When self-assembly meets biology: luminescent platinum complexes for imaging applications, Chem. Soc. Rev., 2014, 43, 4144. DOI: 10.1039/c3cs60453e

- A. Colombo, F. Fiorini, D. Septiadi, C. Dragonetti, F. Nisic, A. Valore, D. Roberto, M. Mauro, L. De Cola, Neutral NCN terdentate luminescent Pt(II) complexes: their synthesis, photophysical properties, and bio-imaging applications, Dalton Trans., 2015, 44, 8478. DOI: 10.1039/c4dt03165b

- A. Valore, A. Colombo, C. Dragonetti, S. Righetto, D. Roberto, R. Ugo, F. De Angelis, S. Fantacci, Luminescent cyclometallated Ir(III) and Pt(II) complexes with beta-diketonate ligands as highly active second-order NLO chromophores, Chem. Commun., 2010, 46, 2414. DOI: 10.1039/b921971d

- A. Colombo, C. Dragonetti, D. Marinotto, S. Righetto, D. Roberto, S. Tavazzi, M. Escadeillas, V. Guerchais, H. Le Bozec, A. Boucekkine, C. Latouche, Cyclometalated 4-Styryl-2-phenylpyridine Platinum(II) Acetylacetonate Complexes as Second-Order NLO Building Blocks for SHG Active Polymeric Films, Organometallics, 2013, 32, 3890. DOI: 10.1021/om4003472

- E. Rossi, A. Colombo, C. Dragonetti, S. Righetto, D. Roberto, R. Ugo, A. Valore, J.A.G. Williams, M.G. Lobello, F. De Angelis, S. Fantacci, I. Ledoux-Rak, A. Singh, J. Zyss, Tuning the Dipolar Second-Order Nonlinear Optical Properties of Cyclometalated Platinum(II) Complexes with Tridentate N^C^N Binding Ligands, Chem. Eur. J., 2013, 19, 9875. DOI: 10.1002/chem.201301131

- J. Boixel, V. Guerchais, H. Le Bozec, D. Jacquemin, A. Amar, A. Boucekkine, A. Colombo, C. Dragonetti, D. Marinotto, D. Roberto, S. Righetto, R. De Angelis, Second-Order NLO Switches from Molecules to Polymer Films Based on Photochromic Cyclometalated Platinum(II) Complexes, J. Am. Chem. Soc., 2014, 136, 5367. DOI: 10.1021/ja4131615

- J. Boixel, V. Guerchais, H. Le Bozec, A. Chantzis, D. Jacquemin, A. Colombo, C. Dragonetti, D. Marinotto, D. Roberto, Sequential double second-order nonlinear optical switch by an acido-triggered photochromic cyclometallated platinum(II) complex, Chem. Commun., 2015, 71, 7805. DOI: 10.1039/c5cc01893e

- H. Zhao, E. Garoni, T. Roisnel, A. Colombo, C. Dragonetti, D. Marinotto, S. Righetto, D. Roberto, D. Jacquemin, J. Boixel, V. Guerchais, Photochromic DTE-Substituted-1,3-di(2-pyridyl)benzene Platinum(II) Complexes: Photomodulation of Luminescence and Second-Order Nonlinear Optical Properties, Inorg. Chem., 2018, 57, 7051. DOI: 10.1021/acs.inorgchem.8b00733

- M. Fontani, E. Garoni, A. Colombo, C. Dragonetti, S. Fantacci, H. Doucet, J.-F. Soulé, J. Boixel, V. Guerchais, D. Roberto, Novel cyclometallated 5-pi-delocalized donor-1,3-di(2-pyridyl)benzene platinum(II) complexes with good second-order nonlinear optical properties, Dalton Trans., 2019, 48, 202. DOI: 10.1039/c8dt03622e

- Colombo, C. Dragonetti, V. Guerchais, D. Roberto, An excursion in the second-order nonlinear optical properties of platinum complexes, Coord. Chem. Rev. 2021, 446, 214113. DOI: 10.1016/j.ccr.2021.214113

- R.E. Doherty, I.V. Sazanovich, L.K. McKenzie, A.S. Stasheuski, R. Coyle, E. Baggaley, S. Bottomley, J.A. Weinstein, H.E. Bryant, Photodynamic killing of cancer cells by a Platinum(II) complex with cyclometallating ligand, Sci. Rep., 2016, 6, 22668. DOI: 10.1038/srep22668

- H. Shi, G. J. Clarkson, P. J. Sadler, Dual action photosensitive platinum(II) anticancer prodrugs with photoreleasable azide ligands, Inorg. Chim. Acta, 2019, 489, 230. DOI: 10.1016/j.ica.2019.02.016

- L. K. McKenzie, H. E. Bryant, J. A. Weinstein, Transition metal complexes as photosensitisers in one- and two-photon photodynamic therapy, Coord. Chem. Rev., 2019, 379, 2. DOI: 10.1016/j.ccr.2018.03.020

- A. Kobayashi, M. Kato, Vapochromic Platinum(II) Complexes: Crystal Engineering toward Intelligent Sensing Devices, Eur. J. Inorg. Chem., 2014, 4469. DOI: 10.1002/ejic.201402315

- O. S. Wenger, Vapochromism in Organometallic and Coordination Complexes: Chemical Sensors for Volatile Organic Compounds, Chem. Rev., 2013, 113, 3686. DOI: 10.1021/cr300396p

- A. Rodrigue-Witchel, D. L. Rochester, S.-B. Zhao, K. B. Lavelle, J. A. G. Williams, S. Wang, W. B. Connick, C. Reber, Pressure-induced variations of MLCT and ligand-centered luminescence spectra in square-planar platinum(II) complexes, Polyhedron, 2016, 108, 151. DOI: 10.1016/j.poly.2015.12.011

- Q. Zheng, S. Borsley, T. Tu, S. L. Cockroft, Reversible stimuli-responsive chromism of a cyclometallated platinum(ii) complex, Chem. Commun., 2020, 56, 14705. DOI: 10.1039/d0cc06775j

- J. Kalinowski, V. Fattori, M. Cocchi, J. A. G. Williams, Light-emitting devices based on organometallic platinum complexes as emitters, Coord. Chem. Rev., 2011, 255, 2401. DOI: 10.1016/j.ccr.2011.01.049

- E. Rossi, L. Murphy, P. L. Brothwood, A. Colombo, C. Dragonetti, D. Roberto, R. Ugo, M. Cocchi, J. A. G. Williams, Cyclometallated platinum(II) complexes of 1,3-di(2-pyridyl)benzenes: tuning excimer emission from red to near-infrared for NIR-OLEDs,  J. Mater. Chem., 2011, 21, 15501. DOI: 10.1039/c1jm12716k

- W. Mroz, C. Botta, U. Giovanella, E. Rossi, A. Colombo, C. Dragonetti, D. Roberto, R. Ugo, A. Valore, J.A.G. Williams, Cyclometallated platinum(II) complexes of 1,3-di(2-pyridyl) benzenes for solution-processable WOLEDs exploiting monomer and excimer phosphorescence, J. Mater. Chem., 2011, 21, 8653. DOI: 10.1039/c1jm10193e

- E. Rossi, A. Colombo, C. Dragonetti, D. Roberto, R. Ugo, A. Valore, L. Falciola, P. Brulatti, M. Cocchi, J.A.G. Williams, Novel N^C^N-cyclometallated platinum complexes with acetylide co-ligands as efficient phosphors for OLEDs, J. Mater. Chem., 2012, 22, 10650. DOI: 10.1039/c2jm16592a

- E. Rossi, A. Colombo, C. Dragonetti, D. Roberto, F. Demartin, M. Cocchi, P. Brulatti, V. Fattori, J.A.G. Williams, From red to near infra-red OLEDs: the remarkable effect of changing from X = –Cl to –NCS in a cyclometallated [Pt(N^C^N)X] complex {N^C^N = 5-mesityl-1,3-di-(2-pyridyl)benzene}, Chem. Commun., 2012, 48, 3182. DOI: 10.1039/c2cc16399c

- F. Nisic, A. Colombo, C. Dragonetti, D. Roberto, A. Valore, J.M. Malicka, M. Cocchi, G.R. Freeman, J.A.G, Williams, Platinum(II) complexes with cyclometallated 5-pi-delocalized-donor-1,3-di(2-pyridyl)benzene ligands as efficient phosphors for NIR-OLEDs, J. Mater. Chem. C, 2014, 2, 1791. DOI: 10.1039/c3tc32086c

- C.-W. Hsu, K. T. Ly, W.-K. Lee, C.-C. Wu, L.C. Wu, J.-J. Lee, T.-C. Lin, S.-H. Liu, P.-T. Chou, G.-H. Lee, Y. Chi, Triboluminescence and Metal Phosphor for Organic Light-Emitting Diodes: Functional Pt(II) Complexes with Both 2-Pyridylimidazol-2-ylidepe and Bipyrazolate Chelates,  ACS Appl. Mater. Interfaces, 2016, 8, 33888. DOI: 10.1021/acsami.6b12707

- M. Z. Shafikov, A. F. Suleymanova, D. N. Kozhevnikov, B. Konig, Thermally Activated Delayed Fluorescence from Ag(I) Complexes: A Route to 100% Quantum Yield at Unprecedentedly Short Decay Time, Inorg. Chem., 2017, 56, 4885. DOI: 10.1021/acs.inorgchem.7b02002

- K. Tuong, Ly, R.-W. Chen-Cheng, H.-W. Lin, Y.-J. Shiau, S.-H. Liu, P.-T. Chou, C.-S. Tsao, Y.-C. Huang, Y. Chi, Near-infrared organic light-emitting diodes with very high external quantum efficiency and radiance, Nat. Photonics, 2017, 11, 63. DOI: 10.1038/NPHOTON.2016.230

- W.-C. Chen, C. Sukpattanacharoen, W.-H. Chan, C.-C. Huang, H.-F. Hsu, D. Shen, W.-Y. Hung, N. Kungwan, D. Escudero, C.-S. Lee, Y. Chi, Modulation of Solid-State Aggregation of Square-Planar Pt(II) Based Emitters: Enabling Highly Efficient Deep-Red/Near Infrared Electroluminescence, Adv. Funct. Mater., 2020, 30, 2002494. DOI: 10.1002/adfm.202002494

- C. Dragonetti, F. Fagnani, D. Marinotto, A. di Biase, D. Roberto, M. Cocchi, S. Fantacci, A. Colombo, First member of an appealing class of cyclometalated 1,3-di-(2-pyridyl)benzene platinum(ii) complexes for solution-processable OLEDs, J. Mater Chem. C., 2020, 8, 7873. DOI: 10.1039/d0tc01565b

- M. Z. Shafikov, P. Pander, A. V. Zaytsev, R. Daniels, R. Martinscroft, F. B. Dias, J. A. G. Williams, V. N. Kozhevnikov, Extended ligand conjugation and dinuclearity as a route to efficient platinum-based near-infrared (NIR) triplet emitters and solution-processed NIR-OLEDs, J. Mater. Chem. C, 2021, 9, 127. DOI: 10.1039/d0tc04881j

- J. Brooks, Y. Babayan, S. Lamansky, P.I. Djurovich, I. Tsyba, R. Bau, M.E. Thompson, Synthesis and characterization of phosphorescent cyclometalated platinum complexes, Inorg. Chem. 41, 2002, 3055. DOI: 10.1021/ic0255508

- P. Brulatti, V. Fattori, S. Muzzioli, S. Stagni, P.P. Mazzeo, D. Braga, L. Maini, S. Milita, M. Cocchi, Tuning the colour and efficiency in OLEDs by using amorphous or polycrystalline emitting layers, J. Mater. Chem. C, 2013, 1, 1823. DOI: 10.1039/c2tc00448h

- W. A. Tarran, G. R. Freeman, L. Murphy, A. M. Benham, R. Kataky, J. A. G. Williams, Platinum(II) Complexes of NCN-Coordinating 1,3-Bis(2-pyridyl)benzene Ligands: Thiolate Coligands Lead to Strong Red Luminescence from Charge-Transfer States, Inorg. Chem., 2014, 53, 5738-5749. DOI: 10.1021/ic500555w

- S. J. Farley, D. L. Rochester, A. L. Thompson, J. A. K. Howard, J.A.G. Williams, Controlling Emission Energy, Self-Quenching, and Excimer Formation in Highly Luminescent N∧C∧N-Coordinated Platinum(II) Complexes, Inorg. Chem., 2005, 44, 9690. DOI: 10.1021/ic051049e

- J. A.G. Williams, A. Beeby, E.S. Davies, J.A. Weinstein, C. Wilson, An Alternative Route to Highly Luminescent Platinum(II) Complexes: Cyclometalation with N^C^N-Coordinating Dipyridylbenzene Ligands, Inorg. Chem., 2003, 42, 8609. DOI: 10.1021/ic035083+]

- J.R. Lakowicz, Principles of Fluorescence Spectroscopy, Third Edition, Springer, pag. 142.

- K. Tuong Ly, R.W. Chen-Cheng, H.W. Lin,. Y.J. Shiau, S.H. Liu, P.T. Chou, C.S. Tsao, Y.C. Huang, Y. Chi, Near-infrared organic light-emitting diodes with very high external quantum efficiency and radiance, Nature Photon, 2017, 11, 63-68. DOI:10.1038/nphoton.2016.230.

- D. Kim, J.L. Brédas, Triplet Excimer Formation in Platinum-Based Phosphors: A Theoretical Study of the Roles of Pt−Pt Bimetallic Interactions and Interligand π−π Interactions, Journal of the American Chemical Society, 2009, 131 (32), 11371. DOI: 10.1021/ja809924t.